Supporting Information

Adsorptive capture of Cd(II) pollutant from water by a sustainable nanobiosorbent of peanut shell biochar-doped-citric acid

Mohamed E. Mahmoud1,* and Sarah M. Elsayed2

1 Faculty of Sciences, Chemistry Department, Alexandria University, Alexandria, Egypt

2 Department of Modeling and Simulation, Advanced Technology and New Materials Research Institute (ATNMRI), City of Scientific Research and Technological Applications (SRTA-City), New Borg El-Arab City, 21934 Alexandria, Egypt

Received: 26, 07, 2025; Accepted: 07, 10, 2025; Published: 16, 11, 2025

Corresponding Author: Mohamed E. Mahmoud*

E-mail: memahmoud10@yahoo.com

https://doi.org/10.62184/acj.jacj1000202522

Table 1S. Specifications of characterization techniques.

| Characterization | Instrument | Conditions |
| --- | --- | --- |
| FT-IR | BRUKER VERTEX 70 Fourier Transform infrared spectrophotometer | In the range 400–4500 cm−1 |
| SEM | Scanning electron microscopic JSM-6360LA, JEOL Ltd. | A carbon tap was used as a substrate for SEM measurements using an ion sputtering coating device (JEOL-JFC-1100E) |
| TGA | TGA-50-Schimadzu, Japan | TGA was acquired using temperature range 25 – 600 oC at 10 oC/min ramp. |
| pH-meter | Adwa pH-meter | Standard buffers 4.01, 7.00 and 10.00 were utilized in the calibration of Adwa pH-meter which used in the measurements of solutions pH. |